## Slide 1: ATM for Concrete Mix Designs
Rich Giessel, ADOT&PF

## Slide 2: ATM 530
ATM 530 Concrete Mix Design by Maximum Aggregate Density
Scope
This method describes the Maximum Aggregate Density Mix Design procedure for determining the optimum proportions for Portland Cement Concrete both with and without supplemental cementitious materials.

## Slide 3: Significance
Concrete proportions, properties and performance depend on the aggregate that forms most of the matrix of this composite material. Many proportioning methods have been used historically to produce concrete. This method utilizes the maximum aggregate density procedure.

## Slide 4: Combined Aggregate Gradation
Combined Aggregate gradations that plot near the maximum density line on a gradation curve typically require less cementitious material and produce concretes with lower shrinkage than concretes that use open-graded aggregate mixtures.

## Slide 5: Critical Aggregate Properties
Aggregate properties important to concrete mix design include; absorption, apparent, bulk SSD, and bulk specific gravity of each fine & coarse aggregate. Sodium Sulfate Soundness or Freeze/Thaw durability, Deleterious particles, Aggregate hardness (for pavements)
ASR is almost never a problem in Alaska

## Slide 6: Cementitious Materials
Cementitious materials acceptable for concrete shall include; Portland Cement, Class C and F Fly Ash, Ground, Granulated Blast Furnace Slag (GGBF), Silica Fume, and Meta-Kaolin.

## Slide 7: Admixtures
Admixture materials acceptable for concrete shall include, water-reducers, surfactants, viscosity modifiers, air-entrainment, crack reducers, shrinkage reducers, accelerators, retarders, water proofers, surface sealers and hardeners.

## Slide 8: Fibers
Fiber materials are acceptable for reinforcement, shrinkage and crack control in concrete and shall include; steel, stainless steel, synthetic, and alkali-resistant cellulose fibers.

## Slide 9: Internal Curing
Internal curing materials include; expanded shale clay or slate fine aggregates, alkali-resistant cellulose, super-absorbent polymers, and naturally occurring aggregates of volcanic origin meeting ASTM C1761.

## Slide 10: Apparatus
Ovens and hot plates thermostatically controlled to maintain the various required temperatures within ± 3°C (5°F).
Fresh Concrete Testing equipment for Slump, Air, Unit Weight, and Temperature, AASHTO T 119, T 152, T 121, and T 309 respectively.
Water bath with temperature control sensitive to ± 0.2°C (0.5°F) at 23°C (73.4°F) per AASHTO T 85.
Balance or scale: Capacity sufficient for the principal sample mass, readable to 0.1 percent or 0.1 g of the total sample mass and meeting the requirements of AASHTO M 231.
Sieve shaker meeting the requirements of WAQTC FOP for AASHTO T 27/T 11.
Specimen molds, either 4x8” or 6x12” with lid that conform to ASTM C470.
Compression Testing machine meeting the requirements of ASTM C39 and referenced documents.
Surface Resistivity testing apparatus meeting the requirements of AASHTO TP 95.
Restrained Shrinkage testing apparatus meeting the requirements of ASTM C1581.

## Slide 11: Proportioning Concrete
Determine the volume of voids in the combined SSD aggregate.
Determine required entrained air content for exposure conditions and maximum aggregate size.
Determine if fiber reinforcement will be required.
Select w/c ratio based on compressive strength requirements.
Calculate volume of paste required to fill remaining voids and provide desired workability.
Calculate admixture volumes required to produce required entrained-air content and workability.

## Slide 12: Trial Batches, Minimum of 3 or 5?
A minimum of three trial batches for no-air concrete and five trial batches for air-entrained will be required to establish w/c vs. strength and air vs. strength relationships. Typically it is best to begin with no-air concrete to establish w/c vs. strength relationship. If done well and the middle no-air batch falls near the optimum w/c ratio then that batch may also be used in establishing the air vs. strength relationship provided the additional batches are made at the same w/c ratio. The two subsequent air-entrained batches should be made near the upper and lower limits of the specified air content.

## Slide 13: First Trial Batch
Prepare first trial batch and check for workability, under-sanded or over-sanded, entrained-air content.
This may require multiple “First” trial batches

## Slide 14: Subsequent Trial Batches
If first trial batch mix parameters are satisfactory then proceed with two additional trial batches with same volume of paste but higher and lower cement contents (lower and higher w/c ratios respectively)
Make sure high w/c mix falls below minimum compressive strength and lower w/c ratio exceed f’cr.
If the initial trial batch is not near the middle of w/c range then prepare a fourth batch near the optimum w/c ratio.
For air-entrained concrete you will need at least two additional trial batches at optimum w/c ratio to produce the % Air vs. Strength curve.

## Slide 15: Fresh Concrete Properties
            Test for:
            Temperature
            Slump (flow if SCC mix)
            Wet unit weight
            Entrained-air content

## Slide 16: Preparing Concrete Test Specimens for High Performance Concrete
Cast one set of restrained shrinkage specimens for each trial batch per ASTM C1581. Measure and record all data for each set of specimens and include it in mix design report.
Cast 15 test cylinders (4x8)

## Slide 17: Test Cylinders
Cast 15 each 4x8” or 10 each 6x12” test cylinders for compressive strength testing of each trial batch.
For Type I/II cement break 3each 4x8” or 2 each 6x12” specimens at 3, 7, 14, 28 days and hold three specimens for possible break at a later age. (Note: High fly ash content concretes may continue to gain significant strength for several years. Additional test specimens should be cast for these mixes as compressive strength at 56 days, 90 days, 1 year and 2 years may be significant.)
For Concrete made with Type III cement break 3each 4x8” or 2 each 6x12” specimens at 1,2, 3, 7 days and hold three specimens for possible break at a later age.

## Slide 18: Curing of Specimens
            Cure compressive and flexural specimens in fog room or water bath as specified in ASTM C511

## Slide 19: Hardened Concrete Properties
Remove test specimens from molds 24 ± 4 hours after casting. Determine hardened unit weight of all specimens by soaking test specimens in 230 C water for 15 minutes then weighing in water followed by weighing in air at SSD.
Immediately prior to compression testing determine the Resistivity of each specimen by AASHTO TP 95. Record resistivity for each specimen, average each set of readings and include data in mix design report.
When flexural strength is required cast three beams in accordance with ASTM C78. Test at the required age and include data in mix design report.

## Slide 20: Graphing Test Results
Graph the 28 day compressive strength vs. w/c ratio for the no-air trial batches.
Graph the 28 day compressive strength vs. air content and provide the linear equation for the data.
Graph the age vs. compressive strength for the trial batch that falls nearest to the optimum mix design.

## Slide 21: Determine Optimum w/c Ratio
            From 28 day compressive strength vs. air content equation compute loss of strength from no-air test values to optimum air content.
            From the graph of compressive strength vs. w/c ratio adjusted by compressive strength loss due to optimum air content, select w/c ratio that will give mix with required f’cr. This will provide the proportions for a Proof Batch at the selected mix design proportions. (DOT&PF typically requires materials for a proof batch to verify concrete mixes made from material without a previous history.)

## Slide 22: Mix Design Report
The report shall include the following:
Project identification, Source/Supplier of mix and name of the general contractor
Aggregate source(s), quality identification(s), target gradation, blend ratio of individual stockpiles, blended absorption, apparent, bulk SSD, and bulk specific for Coarse and Fine Aggregate Fractions. Other properties that may be specified in the Contract include: fineness modulus of the blended fine aggregate; percent flat and elongated; sodium sulfate soundness of coarse and fine aggregate fractions, or aggregate-silica reactivity (ASR).
Graphical representation on a 0.45 power graph of the combined aggregate gradation with the Lower Specification Limit (LSL) and Upper Specification Limit (USL).
Identification and address of the laboratory that performed the mix design, that laboratories mix design identification number and the signed seal of the professional engineer who reviewed and approved the mix design.

## Slide 23: Duplicate Coarse Aggregate SpG
Formulas: | Description: |  |  | Trial 1 | Trial 2 | Average
A | Oven dry mass in air (g) |  |  | 2869.0 | 2892.6 | 
B | SSD mass in air (g) |  |  | 2907.8 | 2933.5 | 
C | Mass in water (g) |  |  | 1820.8 | 1836.2 | 
T | Temperature, C |  |  | 23.4 | 23 | 
A/(B-C) | Bulk Sp.G (oven dry) |  |  | 2.639 | 2.636 | 2.638
B/(B-C) | SSD Sp.G |  |  | 2.675 | 2.673 | 2.674
A/(A-C) | Apparent Sp.G |  |  | 2.737 | 2.738 | 2.738
100[(B-A)/A] | % Absorption |  |  | 1.35% | 1.41% | 1.38%

## Slide 24: Duplicate Fine Aggregate SpG
Formulas: | Description of data or calculation: |  | Trial 1 | Trial 2 | Average
B | Pyc+ Distilled Water |  | 660.7 | 660.7 | 
 | (from calib) Ave M pw, c (g) |  |  |  | 
S | SSD Soil Mass |  | 500.1 | 500.8 | 
C | Pyc + Distilled Water + Agg |  | 973.7 | 974.5 | 
T | Temperature (23.0 ± 2.0°C) |  | 23.0 | 22.7 | 
A | Oven Dry Mass |  | 493.4 | 495.3 | 
A/(B+S-C) | Bulk Sp.G. (Oven Dry) |  | 2.637 | 2.649 | 2.643
S/(B+S-C) | SSD Sp.G. |  | 2.673 | 2.678 | 2.675
A/(B+A-C) | Apparent Sp.G. |  | 2.735 | 2.729 | 2.732
100(S-A)/A | Absorption |  | 1.36% | 1.11% | 1.23%

## Slide 25: Combined Concrete Aggregate Grading
Nominal Maximum Aggregate Size | 3 | 2-½ | 2 | 1-½ | 1 | ¾ | ½ | ⅜ | No. 4
Sieves |  |  |  |  |  |  |  |  | 
3½″ | 99-100 |  |  |  |  |  |  |  | 
3″ | 93-100* | 99-100 |  |  |  |  |  |  | 
2½″ |  | 92-100* | 99-100 |  |  |  |  |  | 
2″ | 76-90 |  | 90-100* | 99-100 |  |  |  |  | 
1½″ | 66-79 | 71-88 |  | 87-100* | 99-100 |  |  |  | 
1″ | 54-66 | 58-73 | 64-83 |  | 82-100* | 99-100 |  |  | 
¾″ | 47-58 | 51-64 | 55-73 | 62-88 |  | 87-100* | 99-100 |  | 
½″ | 38-48 | 41-54 | 45-61 |  | 57-83 |  | 81-100* | 99-100 | 
⅜″ | 33-43 | 35-47 | 39-54 | 43-64 |  | 60-88 |  | 86-100* | 99-100
No. 4 | 22-31 | 24-34 | 26-39 | 29-47 | 34-54 | 41-64 | 48-73 |  | 68-100*
No. 8 | 15-23 | 16-25 | 17-29 | 19-34 | 22-39 | 27-47 | 31-54 | 39-73 | 
No. 16 | 9-17 | 10-18 | 11-21 | 12-25 | 14-29 | 17-34 | 20-39 | 24-54 | 28-73
No. 30 | 5-12 | 6-14 | 6-15 | 7-18 | 8-21 | 9-25 | 11-29 | 13-39 | 16-54
No. 50 | 2-9 | 2-10 | 3-11 | 3-14 | 3-15 | 4-18 | 5-21 | 6-29 | 7-39
No. 100 | 0-7 | 0-7 | 0-8 | 0-10 | 0-11 | 0-14 | 0-15 | 0-21 | 0-29
No. 200 | 0-2.0 | 0-2.0 | 0-2.0 | 0-2.0 | 0-2.0 | 0-2.0 | 0-2.0 | 0-2.0 | 0-2.5

## Slide 26: Combined Aggregate Calculation
 |  | B L E N D R E Q U I R E D - % |  |  |  |  |  |  |  | 
 |  | 0 | 0 | 3/4" | Pea | Pea - Sand | F. Sand |  |  | 
 |  | 0 | 0 | 45.3 | 16.2 | 38.5 | 0 | 100 |  | 
 |  | ACCUMULATED P E R C E N T P A S S I N G |  |  |  |  |  | B L E N D E D |  | MATERIAL
SIEVE SIZE |  |  |  | 3/4" | Pea | C. Sand | F. Sand | A G G R E G A T E S |  | SPECIFICATION
(us) | (mm) |  |  |  |  |  |  |  |  | 
1-1/2" | 37.5 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | % | 100
1.0" | 25 | 100 | 100 | 100 | 100 | 100 | 100 | 100 | % | 99-100
3/4" | 19 | 100 | 100 | 96 | 100 | 100 | 100 | 98.2 | % | 87-100
1/2" | 12.5 | 100 | 100 | 53 | 100 | 100 | 100 | 78.7 | % | 
3/8" | 9.5 | * | 100 | 32 | 95 | 100 | 100 | 68.4 | % | 60-88
1/4" | 6.3 | * |  |  |  |  |  | 0.0 | % | 
#4 | 4.75 | * | 0 | 12 | 33 | 99 | 99 | 48.9 | % | 41-64
#8 | 2.36 | * | 0 | 3 | 5 | 92 | 97.4 | 37.6 | % | 27-47
#16 | 1.18 | * | * | 2 | 2 | 72 | 96 | 29.0 | % | 17-34
#30 | 0.3 | * | * | * | 1 | 45 | 94.7 | 17.5 | % | 9-25
#50 | 0.3 | * | * | * | * | 14 | 81.3 | 5.4 | % | 4-18
#100 | 0.15 | * | * | * | * | 4 | 29.6 | 1.5 | % | 0-14
#200 | 0.075 | 0 | 0 | 1.3 | 0.7 | 1.7 | 6.7 | 1.4 | % | 0 - 2.0
Amount (lbs) |  |  |  | 11,360 | 4,060 | 9,660 |  | 25,080 | Total Agg on Truck Ticket | 
% Total |  |  |  | 45.3% | 16.2% | 38.5% |  |  |  | 

## Slide 27: Combined Aggregate 0.45 Power
Chart: 0.45 POWER CHART
| 5.814823031727798 | 5.108743174423434 | 4.256699612603924 | 3.762176102386298 | 3.116086507375345 | 2.754074108566122 | 2.01610025396293 | 1.471669879582038 | 1.077325409925042 | 0.794635682240205 | 0.581707367927938 | 0.425834718304737 | 0.3117292599535
 | 100 | 100 | 100 | 98.188 | 78.709 | 68.386 | 48.897 | 37.589 | 28.95 | 17.487 | 5.39 | 1.54 | 1.3568
 | 0 | 100 | 100 | 0 | 0 | 100 | 100 | 0 | 0 | 100 | 100 | 0 | 0 | 100 | 100 | 0 | 0 | 100 | 100 | 0 | 0 | 100 | 100 | 0 | 0 | 100
 | 100 | 0
 | 0 | 0 | -1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | -1

## Slide 28: Strength vs w/c Ratio
Chart: Strength vs. Water / Cement Ratio
| 0.4 | 0.45 | 0.5
3 Day psi | 4540 | 3520 | 2700
7 Day psi | 5900 | 5260 | 4590
14 Day psi | 7120 | 6300 | 5640
28 Day psi | 7700 | 6650 | 6130

## Slide 29: No Air Strength vs Age
Chart: Strength vs. Age
| 3.0 | 7.0 | 14.0 | 28.0
7.0 Sack | 4540 | 5900 | 7120 | 7700
6.5 Sack | 3520 | 5260 | 6300 | 6650
6.0 Sack | 2700 | 4590 | 5640 | 6130

## Slide 30: Strength vs Air Content
Chart: 28 Day Strength vs. % Air for three batches at W/C = 0.400
| 3.0 | 5.1 | 6.6
Strength (psi) vs. % Air | 7330 | 5870 | 4320
Strength (psi) vs. % Air | 7330 | 5870 | 4320

## Slide 31: Y = mx + b
Strength vs. Air % |  | 
W/C Ratio | Air Test % | Strength (psi)
0.400 | 3.0 | 7410
0.400 | 5.1 | 5675
0.400 | 6.6 | 4335

## Slide 32: Strength vs Air, Linear Equation
Y = mx + b |  |  | 
Where: | m = |  | 
 | Slope, Loss of |  | b =
 | psi/1.0 %Air |  | y intercept
 | = -827 |  | = 9893
Compressive Strength 8% Air gives: | = -827(% Air) + = -827(8) + | 9893 psi 9893 = 3277 | psi

## Slide 33: Air-Entrained Strength vs Age
Chart: Strength vs. Age
| 3.0 | 7.0 | 14.0 | 28.0
7.5 Sack | 3860 | 4580 | 5290 | 5810
7.0 Sack | 3720 | 4380 | 4860 | 5280
6.5 Sack | 3400 | 3750 | 4490 | 5040
6.0 Sack | 2800 | 3480 | 3960 | 4340

## Slide 34: Thank You